Product Specification Document

MonoStar Ultra High Solids Floor Finish 						                                                                                                                             Page 1 of 2

CLASSIFICATION:

- Ultra High Solids Floor Finish

SCOPE:

- MonoStar is an ultra high solids floor finish with excellent durability and gloss as well as superior leveling.  Saves time and labor with fewer coats.  Designed for medium to low maintenance routines.

FEATURES AND BENEFITS:

Features

- Fewer coats: two coat scrub and recoat and three-four coat full strip application

- Superior leveling with string mop

- Medium to low burnishing frequency

Benefits

  - Time and labor savings versus conventional systems

  - Excellent application appearance

  - Great option for most customers

USAGE:

FOR INDUSTRIAL USE ONLY

DIRECTIONS FOR USE:

Product Uses

MonoStar can be applied over any conventional resilient finish/sealer. Use in a two-coat scrub and re-coat application or a three-coat full strip application.  For use on resilient and other type natural and man made floors.

- Full Strip Preparation: Strip the floor with an Ecolab brand stripper at the recommended use dilution. Rinse well and let dry.

- Scrub and Recoat Preparation: Deep scrub with an Ecolab brand neutral or alkaline cleaner using a blue pad. Rinse and let dry.

- Sealing the Floor: A sealer is not required with MonoStar on most resilient floors. For porous substrates, such as terrazzo, apply 1-2 coats of Ecolab brand sealer for maximum performance.

Application Method: MonoStar may be applied in either thin, medium, or heavy coats, depending on the application technique.

- Thin coverage: 2000 sq ft. / US gal. (196 m²/3.78 L).

- Medium to heavy coverage: 1000 - 1500 sq ft. / US gal (98-147 m²/3.78 L). The average dry time to walk will be 25-40 minutes; allow approximately 40 minutes between coats.

Maintenance: Dust mop daily. Autoscrub or damp mop with an Ecolab brand cleaner. Prepare floors with Ecolab brand cleaners/maintainers prior to burnishing. Burnish 1-4 days/week.

KEEP FROM FREEZING

PHYSICAL PROPERTIES AND CHEMICAL PROPERTIES:

- Compositional Information	Water	7732-18-5

Tributoxyethyl Phosphate	78-51-3

Diethylene Glycol Ethyl Ether	111-90-0

Zinc Ammonium Carbonate	38714-47-5

Proprietary Emulsion	NJ0129124730107

- Physical state: 	Liquid (Emulsion)

- Color:	White (Light)

- Odor:	Acrylic

- pH:	8-9

- Specific Gravity	1.035 – 1.045

- Solids: 			30%

ENVIRONMENT & SAFETY:

- Hazard Rating 	Health – 1	Fire – 0	Reactivity – 0

- WHMIS	Class D-2B

STABILITY & STORAGE:

- Stable under normal conditions of use and handling.

- Do not mix with anything but water.

- Keep from freezing.

FIRST AID:

KEEP OUT OF REACH OF CHILDREN.

CAUTION: May cause eye irritation.

Precautions: Avoid contact with eyes. Wash thoroughly after handling.

FIRST AID

Eye contact: In case of contact, immediately flush eyes with cool running water. Remove contact lenses and continue flushing with plenty of water for at least 15 minutes. Get medical attention if irritation occurs.

Skin contact: Flush contaminated skin with plenty of water. Wash clothing before reuse.

Inhalation: If inhaled, remove to fresh air.

Ingestion: Do not induce vomiting. Never give anything by mouth to an unconscious person. If irritation persists, get medical attention.

FOR EMERGENCY MEDICAL INFORMATION IN USA OR CANADA, CALL 1-800-328-0026.

FOR EMERGENCY MEDICAL INFORMATION WORLDWIDE, CALL 1-651-222-5352 (USA).

READ MATERIAL SAFETY DATA SHEET BEFORE USING PRODUCT.

This document is available in French upon request

PACKAGING & PRODUCT NUMBERS:

| Size Available | Product Number |
| --- | --- |
| 2.5 U.S. Gallon / 9.46 L | 65910077 |